Table of Contents

# 1	Computational screening of sustainable low-emissivity PVD coatings on soda-lime float glass

Technical report Saint-Gobain Research India Author: Varun Mandy, Research Intern Framework: pvdlowe v0.1.0 — https://github.com/VarunMandy/pvdlowe

## 1.1	Abstract

A computational framework was developed to execute the screening workflow set out in the project brief PVD_Usecase.docx: element screening, thermodynamic stability, optical multilayer modelling, design of experiments and multi-objective ranking, for cost-effective low-emissivity coatings deposited by argon magnetron sputtering.

Applying the framework to the brief produced three classes of result. First, the proposed multi-objective weighting was found to contain four defects, one of which allowed a thickness optimiser to return a design consuming 29% more silver than the incumbent while scoring 100/100. Second, two of the brief’s literature citations could not be matched to any locatable source, and one pivotal measurement was found inconsistent with a model-independent electrodynamic limit. Thermodynamic screening of all fifteen nominated chemical systems confirmed that Ag–Cu possesses no stable ordered compound, supporting the brief’s suspicion of phase separation with first-principles evidence. Third, the design-space search identified a material class and a stack architecture outside the brief’s framing, both of which outperform the proposed candidates: silicon nitride dielectrics improve visible transmittance by up to nine percentage points over AZO, and the composition optimum lies at 5–15 at.% Ag rather than the proposed 70%.

No films were deposited. All performance figures are model outputs. The framework’s own validation identifies its largest error — an approximately eightfold under-prediction of sputtered copper sheet resistance — in the material on which most leading candidates depend. A specified experiment resolving this, with pre-registered decision rules and an automated analysis path, is delivered with the framework.

## 1.2	1. Scope and deliverables

### 1.2.1	1.1 What was asked

The brief proposed a materials-by-design programme for transparent low-emissivity coatings on float glass, centred on a dielectric/metal/dielectric architecture (AZO/metal/AZO) and asking how much silver could be removed while retaining visible transmittance, sheet resistance and far-infrared reflectance.

### 1.2.2	1.2 What was delivered

| Deliverable | Status |
| --- | --- |
| Computational framework implementing the brief’s §21 workflow | Complete — 12,000 lines, 86 tests |
| Element and compound screening | Complete |
| Optical multilayer model (transfer matrix, EN 410 / 673 / 12898) | Complete, validated |
| Thin-film transport model coupled to optics | Complete, uncalibrated — requires §6 experiment |
| Multi-objective scoring with provenance grading | Complete |
| Design of experiments generator | Complete |
| DFT input generation (VASP) | Complete, not executed — requires VASP licence and HPC allocation |
| Materials Project integration | Complete and executed — 15/15 systems retrieved |
| Candidate ranking, 36 architectures | Complete, model outputs only |
| Experimental protocol with pre-registered analysis | Complete, not executed — requires tool access |
| Illuminant sensitivity quantified | Complete (§7.3) |
| Manufacturability constraints | Complete |
| Triple-metal architecture search | Complete — negative result (§5.4) |

Repository, documentation, results and protocols are version-controlled and archived to gs://sg-llamole-pvdlowe/pvdlowe/source/.

### 1.2.3	1.3 What was not done, and why

No depositions were performed. The author did not have sputter tool access during the internship period. The experimental work is therefore specified rather than executed, and the protocol in §6 is written as a handover document that a colleague with tool access can run without further input.

## 1.3	2. The framework

### 1.3.1	2.1 Physical model

Optics. A vectorised transfer-matrix solver handles arbitrary layer counts, complex refractive indices, both polarisations and oblique incidence. Thick glass is treated incoherently. Verified against exact Fresnel reflectance for a bare interface, exact null for a quarter-wave antireflection layer, and energy conservation to 10⁻¹⁰ on absorbing stacks.

Optical constants. Metals use the Lorentz–Drude parameterisation of Rakić et al. (1998), with one deliberate departure: the free-electron damping is re-anchored to DC resistivity rather than taken from the published optical fit. Rakić’s fitted Γ₀ for silver implies ρ ≈ 4.4 µΩ·cm against a true 1.587, because in the visible the Drude term trades off against interband oscillators. Using the published value and then applying a thin-film size-effect multiplier double-counts the same scattering, and inflated modelled emissivity roughly threefold in an early build.

Transport. Full Fuchs–Sondheimer integral for surface scattering, Mayadas–Shatzkes for grain boundaries, and a percolation model below a critical thickness. Critically, the resulting resistivity ratio feeds back into the Drude damping: a film too thin to conduct is automatically a film that reflects poorly. Without this coupling, optimising for transmittance drives the metal thickness to zero and reports an excellent coating.

Standards integration. EN 410 / ISO 9050 for visible and solar transmittance; EN 12898 for normal emissivity, weighted by a 283 K Planck radiance; EN 673 for the hemispherical correction and centre-pane U-value, cross-checked against direct angular integration.

### 1.3.2	2.2 Provenance grading

Every physical quantity carries an evidence grade — MEASURED, LITERATURE, LITERATURE_UNVERIFIED, MP_API, DFT_OWN, MODEL, CALIBRATED, ESTIMATE, HYPOTHESIS — and a guard function refuses to admit HYPOTHESIS-grade values into headline tables without explicit opt-in.

This implements the brief’s own caution (“I would not yet put numerical DFT values for Ag₇₀Cu₂₉Ti₁ into a thesis as if they were established facts”) as a type constraint rather than a footnote, so the distinction survives contact with a spreadsheet.

## 1.4	3. Method audit: the multi-objective weighting

The brief’s §14 specifies criteria and weights for ranking candidates. Encoding that table literally produced a scoring function that did not measure the project’s stated objective. Four issues were identified by the framework’s own diagnostics (pvdlowe check-weights). All are documented decisions in data/targets.yaml; none is a silent change.

### 1.4.1	3.1 Silver consumption carried zero weight

The §14 table contains no line for silver consumption, although §17 and §20 both name minimising it as an objective. In the literal encoding, silver mass was computed, displayed, and reported as the limiting criterion, but contributed nothing to the score.

The thickness optimiser exploited this immediately, returning a 12.84 nm design using 0.135 g/m² of silver — 29% more than the incumbent benchmark — at a score of 100/100.

Correction applied: weight 0.15.

### 1.4.2	3.2 Emissivity and sheet resistance double-count one property

Across the candidate set these correlate at r = 0.996, because both are the free-carrier response of the same metal layer. The §14 weights of 0.25 and 0.15 therefore place 0.40 of the total on a single physical quantity.

Correction applied: sheet resistance weighted 0.0 and reported as a constraint. This should be reversed (with emissivity reduced to 0.15) if the coating is also required to function as a transparent electrode, where sheet resistance is an independent objective.

The same diagnostic flags cost against supply risk (r = 0.993) and silver mass against cost (r = 1.000 — silver dominates metal cost so completely that they are the same quantity in different units).

### 1.4.3	3.3 Targets set at the specification minimum, causing saturation

Derringer–Suich desirability saturates at 1.0 once a target is reached. Setting the visible-transmittance target to 0.80 — the brief’s floor of acceptability — made the criterion flat exactly where candidates differ.

The consequence was measurable: across 181 oxide-thickness combinations clearing T_vis = 0.80, transmittance spanned 0.800 to 0.881 while the score decreased from 74.99 to 73.30. The optimiser satisficed at the specification floor and drove the top oxide to 15 nm, a thickness that would not survive handling.

Correction applied: targets set as aspirations (T_vis 0.90, ε_h 0.02). Re-optimising then returned AZO 25 / Ag 10 / AZO 35 nm at T_vis 0.880 — eight points better on identical silver.

General principle: a desirability target should be an aspiration, not a specification minimum.

### 1.4.4	3.4 The supply-risk band could not discriminate

With floor 8.0 against candidate values of 4.5–7.5, all silver-bearing compositions scored 0.1–0.28 and supply risk was reported as limiting for 12 of 14 candidates.

Correction applied: floor 9.5, target 4.0 — still zeroing indium-bearing ITO, which is the criterion’s purpose.

### 1.4.5	3.5 Aggregation

The brief states its weighting should prevent a candidate “winning simply because it has excellent conductivity while being unacceptable optically”. A weighted arithmetic sum does not achieve this — a candidate scoring zero on one criterion forfeits only that criterion’s weight. A geometric mean does.

Under the corrected weighting the pure-silver benchmark ranks 4th under arithmetic aggregation and 7th under geometric; pure copper ranks 1st and 2nd respectively. These are precisely the two candidates the brief is concerned with comparing. The framework defaults to geometric and reports both.

### 1.4.6	3.6 Note on interpreting the diagnostics

The limiting_criterion field is argmin(desirability) — where a candidate is weakest, not what drives the ordering. Under geometric aggregation, whichever criterion sits nearest its floor is reported as limiting for every candidate. The appropriate test of whether weights are doing work is the weight-sensitivity analysis: before these corrections, one candidate won 97.5% of randomised weightings with a rank standard deviation of 0.16, which indicates the weights had no effect rather than that the result was robust.

## 1.5	4. Evidence audit

Eight literature benchmarks were transcribed from the brief. All eight sources have now been located; none has been read in full text.

| State | Count |
| --- | --- |
| Fully verified (full text read, measurement basis confirmed) | 0 |
| Partial (source identified, figures confirmed against abstract) | 6 |
| Disputed (located sources do not contain the quoted figures) | 2 |
| Not located | 0 |

### 1.5.1	4.1 Two citations could not be supported

The figures 85.4% T_vis / 3.21 Ω/sq / 97% FIR and 78.7% T_vis / 2.7 Ω/sq appear in neither located AZO/Ag/AZO study. A companion PET-substrate paper reports 78.5% with 91% FIR at 10 nm Ag — close to one, but a different substrate and a different figure.

Recommendation: these two entries should not be cited pending identification of their source. Both are flagged disputed in the framework.

A corollary worth recording: these two entries are the model’s three closest agreements (0.3%, 1.0%, 1.2% relative error). Excluding them, the median validation error rises from 14.7% to 30.6%. The framework’s apparent accuracy rested partly on figures that cannot be traced.

### 1.5.2	4.2 A pivotal measurement is physically inconsistent

Applied Surface Science 578 (2022) 152051 reports AZO(40)/Cu/AZO(40) with T_vis 87.7%, R_s 9.96 Ω/sq and ε 0.055. The brief’s §16 concludes from this that a silver-free stack may already meet a low-emissivity target — a conclusion that reframes the entire programme.

The transcription is accurate and the abstract attributes all three values to one sample. However, for a conducting sheet thin compared with the wavelength, far-infrared reflectance is fixed by sheet resistance alone:

r = (n₁ − n₂ − Z₀/R_s) / (n₁ + n₂ + Z₀/R_s),    ε = 1 − r²

with Z₀ = 376.73 Ω. No fitted parameter enters. At 9.96 Ω/sq this gives ε ≥ 0.096; the reported 0.055 would require approximately 5.5 Ω/sq.

Four candidate explanations were tested and eliminated:

| Explanation | Outcome |
| --- | --- |
| Values from different samples | Abstract attributes all three to one sample |
| Transcription error | Confirmed against published abstract |
| Far-IR glass index assumption | Limit is 0.091–0.097 across n = 1.5 to 4.0 |
| Band-limited emissometer (8–14 µm) | Reads 5–8% higher, not lower — moves it the wrong way |

The band-emissometer hypothesis was the most plausible and was tested by implementing band-limited emissivity in the framework. For a Drude metal, reflectance is nearly flat across 5–14 µm and the 283 K Planck weighting already peaks near 10 µm, so restricting the band removes the 5–8 µm region where these stacks reflect slightly less well. Correcting for measurement basis therefore worsens the discrepancy, from 0.58 to 0.53 of the limit.

The same group reports ε = 0.045 at 8.10 Ω/sq and ε = 0.050 at comparable sheet resistance. Three measurements at a consistent 0.57–0.63 of the electrodynamic limit indicates a systematic effect rather than an isolated error.

Untested: hemispherical versus normal basis (which would also raise the reading), instrument calibration, or the two quantities being measured on different areas of one nominal sample.

Recommendation: obtain the full text and establish the measurement basis before §16’s conclusion is used. This is the single highest-value literature action outstanding.

### 1.5.3	4.3 A reported thin-film resistivity that cannot be correct

A 2025 study reports ~10 nm films of Ag at 1.59 µΩ·cm, Ag–Cu at 2.97 and Cu at 20.5, deposited under identical conditions.

| Film | Reported | × bulk | Framework model |
| --- | --- | --- | --- |
| Ag, 10 nm | 1.59 µΩ·cm | 1.00× | 4.44 µΩ·cm (2.79×) |
| Cu, 10 nm | 20.5 µΩ·cm | 12.2× | 7.11 µΩ·cm (4.23×) |

Silver’s electron mean free path is 53 nm; a 10 nm film cannot reach bulk resistivity, and Fuchs–Sondheimer alone forces a ratio above approximately 2. The stated thickness uncertainty (±2.5 nm) does not resolve this: the upper bound is still 1.25× bulk. Under identical deposition, the copper film shows a strong size effect and the silver film shows none.

Consequence for the brief. §7 argues that amorphous Ag–Cu retains unusually good conductivity by comparing 2.97 against 1.59. If the silver baseline is not like-for-like, the comparison should be made against the copper value (20.5), against which the alloy appears sevenfold better — the argument survives in stronger form.

### 1.5.4	4.4 Three factual corrections

- Deposition methods differ across the benchmark set. The AZO/Ag/AZO trilayers used RF magnetron sputtering (§3 implies DC); the AZO single-layer study used medium-frequency sputtering. Film density and resistivity do not transfer between techniques and these sources should not be pooled.

- The AZO visible transmittance is 81.4%, not 82.4%. Resistivity 2.6 × 10⁻³ Ω·cm, hardness 11.4 GPa and reduced modulus 98 GPa are confirmed.

- §7’s resistivity table mixes measurement conventions, per §4.3 above.

### 1.5.5	4.5 What verification confirmed

The Ceramics International study states that far-infrared reflectance was measured by FTIR spectroscopy and sheet resistance by four-point probe — a spectroscopic reflectance directly comparable with the framework’s convention, with no emissometer ambiguity. This is consistent with the model reproducing that benchmark to 0.4%, its closest agreement against a traceable source.

It also independently supports the percolation anchor: silver continuity at 10 nm is confirmed by XRD (200 and 220 reflections), which is structural evidence rather than an inference from a resistivity discontinuity.

## 1.6	5. Design-space results

Thirty-six candidate architectures were evaluated; 58 metal systems screened; a 168-point composition series run across two microstructure models, two dielectrics and two climate profiles.

### 1.6.1	5.1 The composition optimum lies at 5–15 at.% Ag

Eight composition curves were generated with stack geometry re-optimised at every composition (Ag 0–100% in 5% steps).

| Profile | Microstructure | Dielectric | Optimum Ag | Score | Plateau |
| --- | --- | --- | --- | --- | --- |
| Heating | Segregated | Si₃N₄ | 0.05 | 89.3 | 0.00–0.20 |
| Heating | Solid solution | Si₃N₄ | 0.00 | 88.9 | 0.00 |
| Heating | Segregated | AZO | 0.10 | 76.5 | 0.05–0.40 |
| Heating | Solid solution | AZO | 0.00 | 74.4 | 0.00–0.05 |
| Cooling | Either | AZO | 0.00 | 68.2 | 0.00–0.15 |
| Cooling | Either | Si₃N₄ | 0.00 | 67.6 | 0.00–0.10 |

Every curve peaks between 0 and 10 at.% Ag. The brief’s Ag₇₀Cu₃₀ priority composition is outperformed in all eight combinations.

This is a sustainability result, not a performance one. Emissivity and sheet resistance continue improving to 50 at.% Ag (0.0386 and 2.59 Ω/sq, the best in the series). The score declines because silver mass carries weight. The trade is approximately 0.005 in emissivity for an 87% reduction in silver, and it is the correct trade only under the premise that silver consumption matters.

Plateau width is more relevant to process capability than peak position. The segregated/AZO curve is flat from 5 to 40 at.% Ag — a wide composition tolerance. Solid-solution curves are sharp (0–5%).

The unresolved microstructure question loses importance in the dilute regime. At Ag₇₀Cu₃₀ the two hypotheses differ by 9–14 points; at Ag₅Cu₉₅ by 2.5. Designing at 5–15 at.% Ag makes the programme robust to a question that is currently unsettled, rather than dependent on it.

### 1.6.2	5.2 Silicon nitride outperforms AZO on visible transmittance

An initial screen of 58 metal systems at fixed AZO thickness found that only pure silver met the full specification; copper failed on transmittance alone (0.752 against 0.80). Allowing the dielectric to vary changed this:

| Metal | AZO | SnO₂ | TiO₂ | Si₃N₄ |
| --- | --- | --- | --- | --- |
| Cu | 0.755 | 0.795 | 0.786 | 0.845 |
| Cu₉₀Zn₁₀ | 0.772 | 0.808 | 0.780 | 0.836 |
| Ag₇₀Cu₃₀ | 0.837 | 0.869 | 0.835 | 0.912 |
| Ag | 0.880 | 0.902 | 0.868 | 0.923 |

Silicon nitride gains nine percentage points of visible transmittance on copper — the margin that was disqualifying it. All metals improve, indicating a dielectric property rather than a copper-specific effect.

Notably, the highest-index material does not win: TiO₂ (n = 2.45) underperforms SnO₂ (n = 2.00). Antireflection around a metal layer is an index-matching problem, not an index-maximisation problem.

Why this was outside the brief’s framing. The brief’s screening began from the periodic table and the Materials Project, both of which surface oxides. Nitrides fall outside that search structure. Silicon nitride is nonetheless the industry-standard Low-E dielectric — dense, an effective diffusion barrier, and durable through tempering — and it blocks the oxygen ingress that is copper’s dominant degradation pathway, which is precisely why the Cu/Si₃N₄ pairing is attractive and why it does not appear in the AZO literature.

Lattice absorption was checked and found negligible. Si₃N₄ absorbs near 11.7 µm, within the thermal band, so far-infrared phonon oscillators were added to the model. The penalty on the copper stack is +0.0007 in emissivity (1.7% relative), because at 10 µm the copper layer reflects approximately 96% of the incident field and little reaches the nitride.

### 1.6.3	5.3 Climate reverses the ranking

The brief does not specify a climate, and targets.yaml as derived from it does not constrain solar heat gain. That omission encodes a heating-dominated assumption. Adding the EN 410 / ISO 9050 metrics:

g = T_sol + N·A_sol      (N = 0.36 for a coating on surface 2)
LSG = T_vis / g

| Candidate | Heating | Rank | Cooling | Rank | g | LSG |
| --- | --- | --- | --- | --- | --- | --- |
| Si₃N₄/Ag₁₀Cu₉₀/Si₃N₄ | 89.3 | 1 | 50.4 | 20 | 0.760 | 1.16 |
| Si₃N₄/Cu/Si₃N₄ | 88.9 | 3 | 55.5 | 12 | 0.731 | 1.18 |
| AZO/Cu/AZO | 69.6 | 15 | 65.4 | 1 | 0.558 | 1.32 |
| AZO/Ag/AZO (benchmark) | 65.0 | 22 | 53.0 | 17 | 0.646 | 1.35 |

The mechanism is physical, not a scoring artifact. AZO is a transparent conductive oxide: its free carriers give a screened plasma wavelength at 1.25 µm, inside the solar band. Si₃N₄ is a passive insulator, transparent throughout.

| λ (nm) | 1200 | 1600 | 2000 | 2400 |
| --- | --- | --- | --- | --- |
| Transmittance, AZO stack | 0.240 | 0.115 | 0.068 | 0.046 |
| Transmittance, Si₃N₄ stack | 0.509 | 0.259 | 0.151 | 0.099 |

Same 11 nm copper layer in both. The conductive oxide performs solar-control work that a passive nitride cannot. §5.2 read AZO’s near-infrared absorption purely as a transmittance penalty; a substantial part of it is a solar-control benefit that the heating-weighted objective could not see.

For Indian architectural glazing this is decisive, and the recommended material differs from the heating-climate case. A results table should not be circulated without its weighting profile attached.

### 1.6.4	5.4 Single-metal architectures cannot achieve solar control

The best light-to-solar-gain ratio across all 36 candidates is 1.37, against approximately 2.0 for commercial solar-control glazing. Under the cooling profile, no single-metal stack met the transmittance target.

Generalising the framework to n metal layers separated by n+1 dielectrics:

| Architecture | Metal | Dielectric | Geometry (nm) | T_vis | g | LSG | ε_h | R_s |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Single | Cu | AZO | 45/12/45 | 0.738 | 0.558 | 1.32 | 0.0463 | 2.87 |
| Double | Ag | Si₃N₄ | 15/12/60/12/15 | 0.819 | 0.464 | 1.76 | 0.0248 | 1.67 |
| Double | Cu | Si₃N₄ | 59/13/105/13/59 | 0.716 | 0.516 | 1.39 | 0.0244 | 1.33 |

LSG 1.76 against a single-metal ceiling of 1.37 — a 28% improvement.

A single metal film trades transmittance against infrared reflectance along one curve; thickness moves along that curve but not off it. The dielectric between two metal layers introduces an interference degree of freedom, allowing the two metal reflections to cancel in the visible while adding in the infrared. This degree of freedom does not exist with one metal layer at any thickness or composition — the limitation is architectural, and no compositional search could have revealed it.

A third metal layer was tested and is not worth adding. Scanning n = 1, 2, 3 against the cooling profile, the second layer buys a large gain and the third almost none:

| n | Ag/Si₃N₄ LSG | Ag (g/m²) | Cu/Si₃N₄ cooling score |
| --- | --- | --- | --- |
| 1 | 1.33 | 0.115 | 67.3 |
| 2 | 1.76 | 0.252 | 68.9 |
| 3 | 1.81 | 0.315 | 37.2 |

The third layer adds 0.05 in LSG for a 25% increase in silver, and for copper it is actively harmful — transmittance collapses to 0.437 and the cooling score halves. The architecture argument stops at two layers for this specification. Commercial triple-silver products reach LSG ≈ 2.0 using asymmetric layer thicknesses and tuned interlayer spacing that this coarse scan did not explore; that remains open, but it is a fine-optimisation question rather than an architectural one.

Costs are real. Silver consumption doubles, since each layer must independently exceed percolation near 10 nm. Splitting a film also raises resistance: two 12 nm layers are not equivalent to one 24 nm layer, each carrying its own surface scattering. Process complexity rises to five layers.

Of most interest for the Indian application: the double-copper Si₃N₄ stack achieves LSG 1.39 at R_s 1.33 Ω/sq and ε_h 0.0244 with zero silver, scoring 68.9 on the cooling profile — the highest of any candidate evaluated. Its sheet resistance and emissivity are the best figures the framework has produced. Transmittance at 0.716 remains short of 0.80, but the deficit has narrowed from 12 points to 8 and the dielectric search was coarse.

### 1.6.5	5.5 Thermodynamic screening (Materials Project)

All fifteen chemical systems nominated in the brief’s §9 were retrieved and screened for phases within 50 meV/atom of the convex hull.

The central result: Ag–Cu has no stable ordered compound. Two intermediate phases exist and neither lies on the hull:

| Phase | E above hull | Stable |
| --- | --- | --- |
| Cu₃Ag | 0.0904 eV/atom | No |
| CuAg₃ | 0.0857 eV/atom | No |

Ag–Cu is thermodynamically a phase-separating system — which the brief’s §5 suspected from the 13% lattice mismatch, and which is now supported by first-principles data rather than inferred. The magnitude matters: 86–90 meV/atom is well above k_BT at deposition (26 meV at 300 K, 48 meV at 550 K), so the driving force to separate is substantial rather than marginal.

What this does and does not establish. It is an equilibrium statement. A magnetron-sputtered film is quenched from the vapour at effective rates that routinely trap metastable solid solutions, so it does not predict the as-deposited microstructure. It predicts what the film will do on annealing — which is precisely the discriminating experiment of §8.3, and it indicates the direction to expect: resistivity should fall as copper precipitates from a trapped solution.

It also lends thermodynamic support to the segregated microstructure model, under which §5.1’s dilute-silver optimum is strongest.

Ag–Cu is the only nominated binary with no stable intermediate phase:

| System | Entries | Near-hull | Representative phases |
| --- | --- | --- | --- |
| Ag–Cu | 2 | 0 | — (phase-separating) |
| Ag–Ti | 4 | 2 | Ti₂Ag, TiAg |
| Al–Cu | 15 | 10 | Al₂Cu, AlCu, AlCu₃ |
| Cu–Ti | 12 | 8 | TiCu, TiCu₂, Ti₂Cu |
| Al–Zn–O | 4 | 2 | Al₂ZnO₄, Al₁₀ZnO₁₆ |
| Cu–O | 37 | 9 | Cu₂O, CuO, Cu₄O₃ |
| Ag–O | 18 | 11 | Ag₂O, AgO, Ag₃O |
| Ag–Cu–O | 7 | 4 | CuAgO₂, Cu₂Ag₂O₃ |

This adds a mechanism to the dilute-stabiliser finding in §5.7. Both Cu–Ti and Al–Cu are richly intermetallic — eight and ten near-hull phases respectively. A dilute Ti or Al addition to a Cu-bearing film therefore has stable compounds available to form, so on annealing it is more likely to precipitate an intermetallic than to remain in solution acting as a stabiliser. That is a second reason for the ternary underperforming, independent of the conductivity penalty.

Ag–Cu–O is also populated (four near-hull phases including CuAgO₂), which bears on durability: an Ag–Cu film that oxidises has stable ternary oxides available, not merely a mixture of Ag₂O and CuO.

Limitation. The Materials Project holds DFT results for ordered crystalline phases at 0 K. It cannot describe a disordered sputtered solid solution, thin-film optical constants at 10 nm, or interface energies against an amorphous oxide. The framework records this limitation per query rather than leaving it implicit.

### 1.6.6	5.6 Ranked candidates

All 36 architectures were scored under both climate profiles. The two top-ten lists share no candidates. This is the practical form of §5.3: the climate is not a refinement to the ranking, it selects a different design space.

Columns: geometry as bottom/metal/top in nm; g is the EN 410 solar heat gain coefficient; LSG = T_vis/g; “spec” is T_vis ≥ 0.80, R_s ≤ 5 Ω/sq, ε_h ≤ 0.10.

#### 1.6.6.1	Heating-dominated (Northern Europe) — data/targets.yaml

| # | ID | Architecture | Geometry | T_vis | ε_h | R_s | g | LSG | Ag g/m² | $/m² | Score | Spec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | E10e | Si₃N₄/Ag₁₀Cu₉₀/Si₃N₄ (segregated) | 59/10/48 | 0.878 | 0.0456 | 3.13 | 0.760 | 1.16 | 0.015 | 0.12 | 89.3 | yes |
| 2 | E5e | Si₃N₄/Ag₅Cu₉₅/Si₃N₄ (segregated) | 59/11/48 | 0.864 | 0.0428 | 2.98 | 0.732 | 1.18 | 0.008 | 0.07 | 89.3 | yes |
| 3 | N6 | Si₃N₄/Cu/Si₃N₄ | 60/11/50 | 0.859 | 0.0478 | 3.41 | 0.731 | 1.18 | 0.000 | 0.01 | 88.9 | yes |
| 4 | E5 | Si₃N₄/Ag₅Cu₉₅/Si₃N₄ | 59/11/48 | 0.862 | 0.0540 | 3.99 | 0.729 | 1.18 | 0.008 | 0.07 | 86.8 | yes |
| 5 | N7 | Si₃N₄/Cu₉₀Zn₁₀/Si₃N₄ | 60/11/50 | 0.851 | 0.0616 | 4.66 | 0.727 | 1.17 | 0.000 | 0.01 | 85.0 | yes |
| 6 | E10 | Si₃N₄/Ag₁₀Cu₉₀/Si₃N₄ | 59/11/48 | 0.865 | 0.0594 | 4.50 | 0.730 | 1.19 | 0.016 | 0.14 | 84.8 | yes |
| 7 | N8 | Si₃N₄/Cu₉₀Ag₁₀/Si₃N₄ | 60/11/50 | 0.865 | 0.0594 | 4.50 | 0.732 | 1.18 | 0.016 | 0.14 | 84.7 | yes |
| 8 | N35e | Si₃N₄/Ag₆₀Cu₄₀/Si₃N₄ (segregated) | 45/9/40 | 0.904 | 0.0445 | 3.04 | 0.794 | 1.14 | 0.065 | 0.53 | 81.7 | yes |
| 9 | N5 | Si₃N₄/Ag₂₅Cu₇₅/Si₃N₄ | 60/11/50 | 0.874 | 0.0714 | 5.67 | 0.735 | 1.19 | 0.038 | 0.31 | 79.7 | no |
| 10 | N3e | Si₃N₄/Ag₇₀Cu₃₀/Si₃N₄ (segregated) | 25/9/35 | 0.900 | 0.0453 | 3.16 | 0.770 | 1.17 | 0.073 | 0.59 | 79.2 | yes |
| — | M0 | AZO/Ag/AZO (benchmark) | 35/10/35 | 0.876 | 0.0603 | 4.18 | 0.646 | 1.35 | 0.105 | 0.85 | 65.0 | yes |

Every entry uses silicon nitride. Nine of ten meet the full specification; eight of ten use less than 0.05 g/m² of silver against the benchmark’s 0.105. The leading candidate beats the benchmark on transmittance, emissivity and sheet resistance simultaneously while using one seventh of the silver.

#### 1.6.6.2	Cooling-dominated (India) — data/targets_cooling.yaml

| # | ID | Architecture | Geometry | T_vis | ε_h | R_s | g | LSG | Ag g/m² | $/m² | Score | Spec |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | M6 | AZO/Cu/AZO | 35/12/35 | 0.738 | 0.0463 | 2.87 | 0.558 | 1.32 | 0.000 | 0.01 | 65.4 | no |
| 2 | D10e | AZO/Ag₁₀Cu₉₀/AZO (segregated) | 15/9/37 | 0.789 | 0.0585 | 3.52 | 0.641 | 1.23 | 0.013 | 0.11 | 59.3 | no |
| 3 | D15e | AZO/Ag₁₅Cu₈₅/AZO (segregated) | 15/9/37 | 0.794 | 0.0564 | 3.31 | 0.643 | 1.23 | 0.019 | 0.16 | 59.3 | no |
| 4 | S10 | ITO/Ag₇₀Cu₃₀/ITO | 35/10/35 | 0.852 | 0.0688 | 5.48 | 0.620 | 1.37 | 0.081 | 0.66 | 58.3 | no |
| 5 | M5 | AZO/Ag₂₅Cu₇₅/AZO | 35/10/35 | 0.784 | 0.0780 | 5.92 | 0.612 | 1.28 | 0.034 | 0.28 | 58.2 | no |
| 6 | M3ema | AZO/Ag₇₀Cu₃₀/AZO (segregated) | 35/10/35 | 0.840 | 0.0462 | 2.63 | 0.635 | 1.32 | 0.081 | 0.66 | 57.9 | yes |
| 7 | M35e | AZO/Ag₆₀Cu₄₀/AZO (segregated) | 15/9/35 | 0.843 | 0.0514 | 2.95 | 0.659 | 1.28 | 0.065 | 0.53 | 57.4 | yes |
| 8 | D10 | AZO/Ag₁₀Cu₉₀/AZO | 15/9/37 | 0.786 | 0.0784 | 5.66 | 0.638 | 1.23 | 0.013 | 0.11 | 57.1 | no |
| 9 | D15 | AZO/Ag₁₅Cu₈₅/AZO | 15/9/37 | 0.790 | 0.0828 | 6.15 | 0.639 | 1.24 | 0.019 | 0.16 | 56.3 | no |
| 10 | M4 | AZO/Ag₅₀Cu₅₀/AZO | 35/10/35 | 0.809 | 0.0844 | 6.68 | 0.621 | 1.30 | 0.062 | 0.51 | 55.7 | no |
| — | M0 | AZO/Ag/AZO (benchmark) | 35/10/35 | 0.876 | 0.0603 | 4.18 | 0.646 | 1.35 | 0.105 | 0.85 | 53.0 | yes |

Every entry uses a conductive oxide (AZO or ITO), for the reason in §5.3 — the free carriers reject solar near-infrared, which a passive nitride cannot. But only two of ten meet the full specification, and both of those use substantial silver. The rest fail on visible transmittance.

This is the honest state of the cooling-climate answer: the framework is ranking near-misses. No single-metal architecture in the set clears T_vis ≥ 0.80 at acceptable solar gain, which is the finding that motivated the multi-layer work in §5.4. The double-copper Si₃N₄ stack scores 68.9 on this profile — higher than anything in the table above — but at T_vis 0.716 it too falls short.

#### 1.6.6.3	How to read these tables

- They share no candidates. A recommendation is only meaningful with its climate profile named. Circulating one table without the other would be misleading.

- The benchmark appears in neither top ten, which is the correct answer to the brief’s question: pure silver is the incumbent to beat, and on a sustainability-weighted objective it is beaten.

- Four of ten in each list are “segregated” variants — the same composition under the alternative microstructure hypothesis. Until the Phase 2 measurement (§8.3) is made, those four entries are conditional. §5.5 provides thermodynamic support for segregation but not proof of the as-deposited state.

- All copper-bearing entries are contingent on §6. The framework under-predicts sputtered copper sheet resistance by roughly eightfold; if that gap is real film quality rather than model error, most of both tables is affected.

- Scores are not comparable between the two tables, being computed under different weightings. Compare within a column only.

### 1.6.7	5.7 The dilute-titanium ternary is predicted to underperform

Ag₇₀Cu₂₉Ti₁, proposed in the brief on the hypothesis that dilute Ti stabilises the metal layer, ranks 13th of 14 in the original candidate set. Titanium’s bulk resistivity is 42 µΩ·cm, approximately 26× silver’s; even at 1 at.% this raises alloy resistivity enough to give the worst sheet resistance (7.55 Ω/sq) and worst emissivity (0.0921) in the set. The interfacial benefit may be real, but the conductivity penalty is weighting-independent.

A titanium barrier layer remains the better test of the interface hypothesis, isolating the interfacial effect without placing Ti in the conduction path — as industrial coatings do. It is not, however, a silver-reduction candidate: it uses a full pure-silver layer and ranks last once silver consumption is weighted. The two claims should be kept separate.

## 1.7	6. The critical unknown, and the experiment that resolves it

### 1.7.1	6.1 The discrepancy

Validation against literature shows the model reproducing silver stacks well in the infrared — its intended strength — and failing on copper:

| Benchmark | Metric | Reported | Modelled | Error |
| --- | --- | --- | --- | --- |
| AZO/Ag(13)/AZO | Far-IR reflectance | 0.960 | 0.964 | 0.4% |
| AZO/Cu/AZO (2022) | Sheet resistance | 9.96 | 2.86 | 71% |
| AZO/Cu(15)/AZO | Sheet resistance | 16.6 | 2.10 | 87% |

The model under-predicts sputtered copper sheet resistance by approximately eightfold. The classical size effect cannot account for a gap of this magnitude, which points to a mechanism the model does not contain: oxygen incorporation during deposition, native oxide at the interfaces, or substantially poorer grain structure than silver on the same underlayer.

If this reading is correct, the obstacle to the copper route is film quality rather than intrinsic physics — an engineering problem with known levers (base pressure, seed layers, getter, substrate temperature) rather than a fundamental limit. That is a considerably more tractable target than replacing silver’s electronic structure.

It also gates six of the leading candidates in both climate profiles.

### 1.7.2	6.2 The experiment

Specified in experiments/BENCH_cu_series.md with pre-registered decision rules in experiments/PROTOCOL_cu_series.md.

Matrix. Cu at 8, 10, 12, 14, 16, 18, 20 nm plus a 10 nm Ag control, all as AZO(40)/metal/AZO(40) capped trilayers, deposition order randomised. Plus one uncapped Cu film at 12 nm as an oxidation control.

Key design decisions.

Films must be capped. Bare 10 nm copper oxidises in air within minutes, and the hypothesis under test is that oxygen degrades these films. A bare film measured after venting reports air oxidation rather than deposition quality. The framework de-embeds the AZO shunt to recover the metal layer; the correction is non-linear and largest where it matters — a measured 16.6 Ω/sq trilayer is 22.6 Ω/sq in the metal alone, a 36% difference. Omitting it would bias the result toward “the copper is acceptable”.

Order randomised. Target erosion drifts across a campaign; in ascending thickness order that drift aliases directly onto thickness and cannot be separated from a size effect.

Thickness measured independently. ρ = R_s · t, so a 20% thickness error becomes a 20% resistivity error and would be misattributed to a scattering parameter.

Silver control is a stop condition. AZO/Ag(10)/AZO should give approximately 4–5 Ω/sq. If it does not, the tool requires diagnosis before the copper series can be interpreted.

Analysis. One command:

pvdlowe calibrate -i experiments/cu_series_runsheet.csv --capped

This fits specularity, grain-boundary reflection, percolation threshold and a thickness-independent excess resistivity, then diagnoses which of three mechanisms is operating.

### 1.7.3	6.3 Pre-registered decision rules

Written before any data exists, so that interpretation is not selected to suit the outcome.

| Rule | Criterion | Interpretation | Consequence |
| --- | --- | --- | --- |
| A | Excess < 1 µΩ·cm, ρ(100 nm)/ρ_bulk < 1.5 | Classical size effect; model form correct, parameters wrong | Adopt fitted parameters; copper recommendations stand with revised figures |
| B | Excess > 50% of bulk, improving fit by > 20% | Impurity scattering, most likely oxygen | Favourable: film quality, not physics. Follow with base-pressure study and XPS depth profile |
| C | Fitted d_c differs from 11 nm by > 1.5 nm | Dewetting on this underlayer | Minimum usable thickness changes, and with it every silver-consumption figure. Trial a seed layer |
| D | R_s at 15 nm near 16.6 Ω/sq | Literature is correct; model optics optimistic by ~8× | Six leading candidates fall. Programme reverts to silver reduction, with §5.1’s dilute-silver optimum as the recommendation in its own right |

### 1.7.4	6.4 Validation of the analysis path

The fitter was tested against synthetic data generated with known parameters. All four cases were diagnosed correctly at 0.5–2.4% relative residual, and the percolation threshold was recovered to better than 1 nm in every case.

A limitation identified by that testing and stated in the protocol: specularity and grain-boundary reflection are not separately identifiable from R_s(d) alone — across an 8–20 nm window they produce nearly the same 1/d dependence. A synthetic film generated with p = 0.35 was fitted at p = 1.00 with a 1.5% residual: an excellent fit to the data and an incorrect value for the parameter.

The fitted model therefore predicts sheet resistance reliably within the fitted range, which is what the framework requires, but the individual parameters must not be reported as measurements. Separating them requires varying grain size independently, for instance by annealing at fixed thickness. The percolation threshold is identifiable, and is the parameter of greatest consequence since it sets minimum usable thickness.

## 1.8	7. Limitations

### 1.8.1	7.1 No experimental validation

No films were deposited. Every performance figure in this report is a model output. The candidate rankings are hypotheses ordered by physics, suitable for directing experimental effort, and are not results.

### 1.8.2	7.2 Calibrated and fitted parameters

| Parameter | Basis |
| --- | --- |
| Glass far-IR oscillator scale | Calibrated to bare-glass ε_n = 0.837 |
| TCO band-edge strength | Calibrated to n(550 nm) |
| Ag percolation d_c = 10 nm | Literature, XRD-confirmed |
| Cu percolation d_c = 11 nm | Literature, unconfirmed |
| Drude damping | Anchored to DC resistivity |
| Specularity, grain-boundary reflection | Fitted, not measured |

### 1.8.3	7.3 Known weaknesses

- Si₃N₄ and TiO₂ optical constants are ESTIMATE grade — indices from typical sputtered values, phonon parameters order-of-magnitude.

- D65 and AM1.5 spectra are Planckian approximations, flagged as MODEL. The cost of this has now been quantified rather than left open (illuminant_sensitivity): varying the assumed colour temperature over 5000–7500 K moves T_vis by 0.1% and T_sol by 8.3%. The asymmetry is structural — the photopic response V(λ) is narrow and dominates the visible weighting, whereas in the solar band the spectrum is the weighting.

- Consequence: T_vis is reportable as computed. T_sol, and the g-value and LSG derived from it, carry a systematic uncertainty of order 5–10% until a tabulated AM1.5G spectrum is supplied. Rankings within a climate profile are unaffected, the bias being common to all candidates, but absolute solar-gain figures quoted against a building code are.

- Visible-range metal optics are accurate to a few per cent at best. The far-infrared response is reliable, being pure Drude and anchored to resistivity; the visible is not.

- Roughness, interdiffusion and barrier absorption are not modelled. A real stack will transmit somewhat less than predicted.

- Reactive Si₃N₄ deposition is more demanding than AZO — target poisoning, lower rate. The brief’s §15 deposition-efficiency criterion would penalise it, and the framework cannot score this without a calibrated rate model.

### 1.8.4	7.4 Scores are not portable between weightings

Absolute scores moved by approximately 25 points as the §3 corrections were applied. A score is not a property of a material. A figure of 89.3 is a statement about one architecture under one weighting of eight criteria, three of which the framework cannot populate. Rankings should be quoted with the weighting file attached and the unverified elements identified.

## 1.9	8. Recommendations

### 1.9.1	8.1 Immediate — literature

- Obtain the full text of Applied Surface Science 578 (2022) 152051 and establish whether the reported emissivity is normal or hemispherical, and the instrument’s spectral band. §16’s conclusion depends on this.

- Withdraw the two disputed citations (§4.1) from any document derived from the brief pending identification of their source.

- Apply the three factual corrections in §4.4.

### 1.9.2	8.2 First experimental priority

Execute the copper thickness series (§6). Half a day of tool time. It confirms or refutes six leading candidates and is the single highest-leverage measurement available. The protocol is written for handover and requires no further specification.

### 1.9.3	8.3 Second experimental priority

One AZO/Ag₇₀Cu₃₀/AZO film at 10 nm, sheet resistance measured. The two microstructure hypotheses predict 6.4 versus 2.6 Ω/sq — far outside probe resolution. Better still, measure across Ag 0, 25, 50, 75 at.%: the curve shape is diagnostic, with the segregated model predicting a flat ~3 Ω/sq and a metastable solid solution predicting a Nordheim maximum above 7 Ω/sq.

### 1.9.4	8.4 First deposition run for the target application

For a cooling-dominated application (Indian architectural glazing): AZO/Cu/AZO at 45/12/45 nm, measured for T_vis, sheet resistance and FTIR emissivity, against an AZO/Ag/AZO control.

For a heating-dominated application: Si₃N₄/Cu/Si₃N₄ at 60/12/50 nm against the same control.

Either comparison tests the dielectric hypothesis, the copper film-quality question and the silver-free premise simultaneously.

### 1.9.5	8.5 Framework extensions worth the effort

- Finer optimisation of the double-copper stack — asymmetric outer layers, mixed-metal pairing, finer dielectric steps. The transmittance deficit is 8 points and the scan performed was coarse. This is the most likely route to closing it, now that the triple-layer route has been ruled out (§5.4).

- A tabulated AM1.5G spectrum, to remove the 5–10% systematic on T_sol, g and LSG.

- Measured n and k for in-house AZO, Si₃N₄ and metal films — the largest single source of visible-range error.

## 1.10	9. Handover

| Item | Location |
| --- | --- |
| Source, documentation, results | github.com/VarunMandy/pvdlowe |
| Archive | gs://sg-llamole-pvdlowe/pvdlowe/source/ |
| Executive summary | docs/SUMMARY.md |
| Full findings | docs/FINDINGS.md |
| Physics and approximations | docs/METHODOLOGY.md |
| Evidence grading | docs/PROVENANCE.md |
| Experimental programme | docs/ROADMAP.md |
| Bench procedure | experiments/BENCH_cu_series.md |
| Pre-registered decision rules | experiments/PROTOCOL_cu_series.md |
| Blank run sheet | experiments/cu_series_runsheet.csv |
| Worked example output | experiments/EXAMPLE_filled_runsheet.csv |

Installation is pip install -e .; the test suite (86 tests, no external dependencies beyond numpy/scipy/pandas/pyyaml) runs with python tests/run_tests.py and should be run after any environment change, as it validates the physics rather than only the interfaces.

## 1.11	10. Conclusion

The framework delivered implements the brief’s proposed workflow and, in doing so, identified several respects in which the brief’s own assumptions do not survive quantitative examination: a weighting scheme that omitted the programme’s primary objective, two citations that could not be traced, a measurement inconsistent with a model-independent physical limit, and a material class and stack architecture excluded by the search framing but outperforming the proposed candidates.

The candidate rankings produced should be treated as hypotheses for experimental prioritisation. Their principal weakness is known, quantified, and addressed by a specified experiment with pre-registered decision rules — which is offered as the more useful deliverable. A model that identifies the measurement capable of falsifying it is more valuable to an experimental programme than one that does not.

The recommended next action is half a day of sputter tool time.